COMPOSITE DECKING – TREX SELECT

Part 1 General

  - Section Includes

- Composite Decking (Trex Select)

  - Related Sections

- Section 06-1100 – Wood Framing

  - References

- ASTM D-7032-04: Standard Specification for Establishing Performance Ratings        for Wood-Plastic Composite Deck Boards and Guardrail Systems (Guards or Handrails), ASTM International.

- ASTM D-7031-04: Standard Guide for Evaluating Mechanical and Physical Properties of Wood-Plastic Composite Products, ASTM International

- ASTM E-84-01: Test Method for Surface Burning Characteristics of Building Materials, ASTM International.

- ASTM D 570: Water Absorption of Plastics

- ASTM D 1761: Mechanical Fasteners in Wood

- ASTM D -1413-99: Test method for Wood Preservatives by Laboratory Soil-block Cultures

- ASTM C177: Standard Test Method for Steady-State Heat Flux Measurements and Thermal Transmission Properties by Means of the Guarded-Hot-Plate Apparatus

  - Design/Performance Requirements

- Structural Performance:

  - Deck: Uniform Load – 100lbf/sq.ft.

  - Tread of Stairs: Concentrated Load: 750 lbf/sq.ft., and 1/8” max. deflection with a concentrated load of 300 lbf on area of 4 sq. in.

- Fire-Surface Burning Characteristics per ASTM E-84.

  - Submittals

- Product Data Indicate sizes, profiles, surface style, and performance characteristics

- Samples: For each product specified, one sample representing actual product color, size, and finish.

  - Delivery, Storage, and Handling

- Store Trex products on a flat and level surface. Adjust support blocks accordingly

- Support Trex bundles on supplied dunnage

- When stacking Trex bundles, supports should start approximately 8” from each end and be spaced approximately 2ft on center.  Supports should line up vertically/perpendicular to the decking product.

- Do not stack Trex Select decking more than 14 bundles.

- Keep material covered using the provided bundle cover until time of installation.

- See www. Trex.com for detailed storage recommendations;

  - http://s7d4.scene7.com/is/content/Trex/Installation%20Guide%202013pdf

  - Warranty

- Provide manufactures warranty against rot, decay, splitting, checking, splintering, fungal damage, and termite damage for a period of 25 years for a residential installation and 10 years for a commercial installation. In addition provide the Trex Fade and Stain Warranty against food staining and fading beyond 5 Delta E (CIE units) for a period of 25 years for a residential installation and 10 years for a commercial installation. Specific terms for warranties can be found at; www.Trex.com.

Part 2 Products

2.1 Manufacturers

- Contract Documents are based on products supplied by; Trex Company, Inc., 160 Exeter Dr., Winchester, VA 22603.

- Substitutions: Not permitted under Division 01

  - Applications/Scope

- Wood-Plastic Composite Lumber;

  - Material Description: Composite Decking consisting of recycled Linear Low Density Polyethylene (LLDPE) and recycled wood. The product is extruded into shapes and sizes as follows:

    - Trex Select Decking Boards; 0.875” x 5.5”.

    - Lengths – 12, 16, and 20 feet

    - Color – To be specified by owner from Trex’ standard list of colors.

  - Physical and Mechanical Properties as follows:

| Test | Test Method | Value |  |
| --- | --- | --- | --- |
| Flame spread | ASTM E 84 | 85 |  |
| Thermal Expansion | ASTM D 1037 | 1.9 x 10-5 inch/inch/degreeF |  |
| Moisture Absorption | ASTM D 1037 | < 1.2% |  |
| Screw Withdrawal | ASTM D1761 | 388 lbs/in |  |
| Fungus Resistance | ASTM D1413 | Rating - no decay |  |
| Termite Resistance | AWPAE1-72 | Rating = 9.7 |  |
|  |  | Ultimate (Typical)Values * | Design Values |
| Compression Parallel | ASTM D198 | 1588 psi | 540 psi |
| Compression Perpendicular | ASTM D143 | 1437 psi | 540 psi |
| Bending Strength | ASTM D198 | 3280 psi | 500 psi |
| Shear Strength | ASTM D143 | 1761 psi | 360 psi |
| Modulus of Elasticity | ASTM D4761 | 400,000psi | 200,000 psi |
| Modulus of Rupture | ASTM D4761 | 3750 psi | 500 psi |

* Ultimate strength values are not meant for design analysis. Design values are for temperatures up to 130F (54C)

  - Accessories

- Fasteners:

  - Trex Universal Hideaway Hidden Fasteners

  - Screws; See - http://s7d4.scene7.com/is/content/Trex/Installation%20Guide%202013pdf for the updated recommendations on fasteners.

Part 3 Execution

3.1 Installation

A.  Install according to Trex installation guidelines. http://s7d4.scene7.com/is/content/Trex/Installation%20Guide%202013pdf

B.   Cut, drill, and rout using carbide tipped blades

C.   Do not use composite wood material for structural applications

3.2 Cleaning

A.  Following cleaning recommendations as found in Trex installation guide at;

http://s7d4.scene7.com/is/content/Trex/Installation%20Guide%202013pdf